Iodine Doping Facilitates the Phase Formation of Lithium-Argyrodite Solid Electrolyte

Abstract: All-solid-state lithium batteries (ASSLBs) with solid-state electrolytes (SSEs) have attracted wide attention for their high energy density and reliable safety performance. Halogen-substituted lithium argyrodites, Li6PS5Cl (LPSC), represent class of promising and suitable sulfide-based solid electrolytes with high conductivity and great processability. In the mass production process of simple high-speed mixing of raw materials without treatment, however, obtained LPSC electrolyte will still exist Li2S raw material signal. Herein, in this study, introducing LiI to argyrodite LPSC electrolyte is proposed to reduce the raw material phase of Li2S and enhance ionic conductivity (up to 3.91 mS·cm-1). Moreover, iodization of the argyrodite LPSC is found lower the crystallization temperature of LPSC. By combining Li6PS5Cl0.95I0.05 (I0.05-LPSC) with a graphite (Gr) anode and a NCM622 cathode, a room temperature ASSLBs with excellent long-term cycling stability (97.9% capacity retention at 0.3 C for 100 cycles) and a high reversible capability (134.8 mAh·g-1 at 0.3 C) is reported. These results prove that the doping of LiI can reduce the difficulty of synthesis of argyrodite.

Keywords: lithium argyrodites, Li6PS5Cl, Li2S raw peak, LiI, ionic conductivity, solid state battery

- Introduction

Lithium-ion batteries (LIBs) have occupied the consumer electronics market, dominating the lead in electric vehicles, and energy storage[1-7]. Due to the flammable property of organic electrolytes, commercial lithium-ion batteries suffer a serious thermal runaway problem, which prevents its further application and development[8-10]. All-solid-state lithium batteries (ASSLBs) with non-flammable inorganic solid electrolytes are promising alternatives to the safety problem. Solid state electrolytes (SSEs) have significantly drawn attention due to their wide electrochemical voltage window, excellent thermal stability, good manufacturing performances, wide operating temperature range, and superior safety[11-13].

Specifically, sulfide solid electrolytes are strong candidates for all-solid-state batteries due to their high ionic conductivity compared to other electrolytes[14, 15]. The argyrodites Li6PS5X (X = Cl, Br) with high ionic conductivity of∼10-3 S cm-1 and low cost owing to the utilization of cheap synthesis precursors are widely studied in recently years, which is a representative in sulfide solid electrolytes[16, 17]. Some previous studies have demonstrated that their conductivities are affected by lithium vacancy concentration and structural disorder between the S2-/X- positions[18-20]. Among them, several reports have been published on the enhancement of conductivity by cationic and anion doping[16, 21, 22].

In a general way, the most widely used method of preparing sulfide SSEs is high-energy ball milling followed by annealing. The high-energy ball milling process is time-consuming and the yield is low[23-26], which is not reliable for mass production. If the direct mixing method is used, large particle size of precursor will lead to a residual Li2S signal[27]. These residua Li2S can cause the conductivity of the electrolyte to still not be high enough. In previous research, Ujiie Satoshi et al. [28] reported that addition of LiI decreased the intensity of the X-ray diffraction (XRD) peak attributable to 70Li2S·30P2S5 glass–ceramic and improved the ionic conductivity.

In this work, completely untreated raw materials are used, and all the raw materials are simply mixed and then sintered. After doping LiI, the sintering temperature is reduced (550 to 480℃), and the Li2S raw material peak in electrolyte is less. The Li6PS5Cl0.09I0.05 electrolytes present the high room temperature ion conductivity of 3.91 mS·cm-1. In-situ X-ray diffraction (in-situ XRD) was used to monitor the sintering process, it was found that the phase forming temperature of argyrodite decreased. Finally, the NCM622/ Li6PS5Cl0.95I0.05 /graphite ASSLBs was used to study the electrochemical properties of Li6PS5Cl0.95I0.05 electrolyte.

- Experimental Section

  - Preparation of solid electrolytes

To prepare Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolytes, Li2S (99.98%, GanFeng Lithium Co., Ltd.), P2S5(99%, P > 24 wt%, Sinopharm Chemical Reagent Co., Ltd.), and anhydrous LiCl (99.98%, dried at150 ℃, <200 ppm, Aladdin) crystalline powders were weighed according to a certain stoichiometric ratio of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4). Then the 20g raw materials were pulverized at ultra-high speed (25000 rpm) with a powder-mixing machine (DaDeYaoJi)[27]. The precursor powder sample with uniform particle sizes can be obtained in 150 s by a total of 6 stirring times (25 s per time), following 1 minute interval each time for heat dissipation of the powder-mixing machine. The obtained precursor powder was sealed in a quartz bottle and annealed at 480 °C (heating rate of 2 ℃ min-1) for 10 h and then naturally cooled to obtain the final Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolytes. All the above operations were carried out under an argon atmosphere.

  - Materials characterization

Powder XRD patterns were collected using an Ultima IV. XRD cells containing hermetically sealed SSE samples with a polyimide (PI) film were mounted on an XRD diffractometer and measured at 40 kV and 40 mA from 10 ° to 70 ° with a scan speed of 2.4 ° min-1. The powder was tested by XRD in situ, and the test temperature was 25-550 ℃, and the sample was taken every 30 ℃, and the holding time at each temperature point was 30 min. Rietveld refinements of Powder XRD data were conducted using Fullprof software. X-ray photoelectron spectroscopy (XPS) was performed by PHI 5000 Versa Probe III with a monochromatic Al Kα X-ray source with a beam size of 200 um using inert-atmosphere protected transferring device. The observed binding energies were calibrated with the adventitious C1s peak to 284.8 eV. Scanning electron microscopy (SEM, TESCAN MIRA3) equipped with an energy dispersive spectroscopy (EDS, Bruker) addon was adopted to characterize the morphologies and elemental distributions, respectively. Raman spectra were measured with AW200SG, Electrotek Raman spectrophotometer (UK) in the range of 50-450 cm-1, using an Ar ion laser beam and an excitation wave length of 514 nm.

  - Electrochemical characterization

The ionic conductivity of the Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolyte material was analyzed by AC impedance spectroscopy. The tested electrolyte pellets were obtained by pressing 300 mg of electrolyte powder into a pellet with a 10 mm diameter under a pressure of 1.25 tons. The carbon-coated aluminum foils were placed on both sides of the electrolyte pellet as the blocking electrode. AC impedance test was carried out using Ivium electrochemical workstation in the frequency range of 1 Hz to 1 MHz with an applied voltage of 0.2 V. The In/ SSEs /In symmetric batteries are used for EIS at different temperatures, which vary continuously from low to high temperature (-15~75 ℃) by Toyo Co. Ltd. LN-Z2-HF.

All solid-state NCM622/I0.05-LPSC/Gr mold batteries were assembled in the following manner. Commercial NCM622 and I0.05-LPSC electrolyte were prepared in a weight ratio of 7:3 into a mixer for high-speed mixing (Thinky mixer ARE310) at a speed of 1000 rpm for 150 s to obtain the final composite cathode. The preparation process of the composite anode is similar to that of the cathode, except that the weight ratio of graphite and electrolyte is 6:4. During the assembly of the full battery, we first obtain electrolyte pellets by pressing 100 mg of electrolyte powder into a pellet with a 10 mm diameter under a pressure of 1.25 tons. Then 21 mg of the above-mentioned cathode was used in combination with 100 mg of I0.05-LPSC electrolyte to make a 10 mm two-layer pellet by a pressure of 1.9 tons. Next, a pressure of 2.5 tons was applied to make the three-layer pellet followed by attaching 14 mg anode mixture on the other side. Finally, we assembled the battery into a mold. All the electrochemical properties measurements for solid-state lithium batteries in this work are performed at room temperature.

- Results and Discussion

Figure 1. (a) Measured X-Ray diffraction patterns of the as-prepared Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) samples and the magnified angle on the right shows the main peak of lithium sulfide. (b) Raman spectra of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) samples. (c) XRD pattern of and the corresponding Rietveld refinement of Li6PS5Cl0.95I0.05 sample. (d) Structural representation of the Li6PS5Cl0.95I0.05 samples.

Figure 1a depicts XRD patterns of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolytes, the main peaks at 30° could be indexed as cubic argyrodite phase (F-43m)[29], indicate that the argyrodite electrolyte with fast ion channels can be synthesized in this way. However, there is a raw material peak of Li2S in the LPSC phase, and after doping LiI, the peak intensity of Li2S gradually decreases with the increase of the amount of incorporation. But if the doping is too much (x > 0.1), the main peak splitting will occur due to the phase change caused by the lattice constant. In addition, Figure 1b shows the Raman spectroscopy results of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolyte, indicating that the peak at 425 and 568 cm− 1 corresponds to the PS43 − group, which further testify the argyrodite structure[30]. Besides, with the I concentration increased, the main PS43 − unit appear no split and slightly shifts the wave number towards the lower direction (red shift)[31, 32]. These results indicate that I entered the lattice of S-Cl of the argyrodite structure.

In order to gain a deeper understanding of the impact of doping, XRD Rietveld refined of Li6PS5Cl0.95I0.05 sample was used. The fitted pattern and refined pattern parameters are shown in Figure 1c and Table S1, respectively. On account of the large radius of I than that of Cl, the appearance of the lattice expansion phenomenon is detected by the refined larger lattice parameter of a=9.874Å, with comparison to a=9.858Å for Li6PS5Cl structure (Figure S1 and Table S2). The Rietveld analysis also suggests that the incorporated I atoms share the 4a/4c site with Cl atoms and present an occupation ratio of 4.99%, which is very close to 5% doping amount of previous design. Figure 1d shows the crystal structure of Li6PS5Cl0.95I0.05, in which the Cl-/I- anions form a face centered cubic lattice (Wyckoff positions 4a and 4c), with S2- anions in half of the tetrahedral voids and PS43- tetrahedra on the octahedral sites (P on Wyckoff 4b).

Figure 2. (a) Measured I 3d XPS spectra of Li6PS5Cl1-xIx (x=0, 0.05) samples. (b) EDS mapping of Li6PS5Cl0.95I0.05 electrolyte pellet.

The prepared solid electrolyte was examined using XPS spectra. Figure S2a depicts the deconvolution spectra of the Li1s region of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolytes, and one sharp peak is clearly visible at 55.68 eV, which is correlated to Li1s from argyrodites. Also, the P 2p and S 2p spectra of the electrolytes show the characteristic signals for PS43- tetrahedra[33]. Additionally, the XPS spectrum of the precursor LiI for I 3d is at 618.90 eV[34], and Li6PS5Cl0.95I0.05 electrolyte for I 3d appears at 618.18 eV, which is consist with the XPS spectrum of Li6PS5I[35]. These results indicate that the chemical state of I 3d has changed and the substituted I element existed in the LPSC structure. EDS mapping images of I0.05-LPSC and LPSC electrolyte pellet in Figure 2b and Figure S3b, I element was evidently detected in the EDS mapping of I0.05-LPSC, where P, S, Cl, and I were uniformly distributed. Furthermore, I0.05-LPSC electrolyte powder shows in Figure S3a, in which most of electrolyte particles display small and uniform particle size (<10 μm).

Figure 3. (a) Ionic conductivities measured at 28 ℃. (b) Nyquist plots and the fitting plots, and (c) Arrhenius plots of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4).

The LPSC electrolyte is synthesized in Figure S4, and the sintering temperature needs to 550°C to achieve ionic conductivity of 4.3 mS·cm-1. Because the melting point of LiI is lower (469 °C), the electrolyte prepared in this study can obtain a high conductivity when the sintering temperature is 480 °C. The Li+ conductivities of electrolyte were measured using cold-pressed pellets. Figure 3a shows the ionic conductivities of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) electrolytes. Clearly, the highest room temperature conductivity of 3.91 mS·cm-1 was obtained by Li6PS5Cl0.95I0.05. Conductivities of Li6PS5Cl1-xIx electrolytes with x=0, 0.1, 0.2, 0.3, 0.4 are 3.47, 3.51, 2.74, 1.62 and 0.61 mS·cm-1, respectively. The corresponding Nyquist plots are presented in Figure 3b and the fitting parameters for Li6PS5Cl1-xIx impendence spectra are shown in Table S3. The activation energy (Ea) was calculated using the equation σT=σ0exp(-Ea/kBT), where σ represents the Li+ conductivity, σ0 denotes a pre-factor, T represents the absolute temperature, and kB is the Boltzmann constant[36]. The Arrhenius plots of the Li6PS5Cl1-xIx in the temperature range from -15 to 75 °C are depicted in Figure 3c, and the calculated activation energy values of Li6PS5Cl1-xIx electrolytes with x = 0, 0.05, 0.1, 0.2, 0.3,0.4 are 0.3958, 0.3972, 0.3783, 0.3838, 0.4117 and 0.3959 eV, respectively. Figure S5 shows the EIS results of Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2, 0.3, 0.4) under different temperatures.

Figure 4. Details from in-situ XRD patterns at various temperatures for (a) Li6PS5Cl and (b) Li6PS5Cl0.95I0.05.

According to the results of the conductivity result, the doping limit was reached at Li6PS5Cl0.8I0.2. Therefore, Li6PS5Cl1-xIx (x=0, 0.05, 0.1, 0.2) precursor mixture was subjected to in-situ XRD test in order to understand the effect of LiI doping on the preparation. Figure 4a shows in situ XRD data recorded during the heat treatment of Li6PS5Cl precursor. With the increase of temperature (25-550 ℃), the characteristic peaks of Li-argyrodite phase appear at 450 ℃ and the peak intensity gradually increases, in addition, the peak intensity of Li2S has maintained a high level. Similarly, the same test conditions were used for the Li6PS5Cl0.95I0.05 in Figure 4b. There are some different situations, the characteristic peak of Li-argyrodite phase began to appear at 100 ℃, became very weak at 300 ℃, but gradually increased after 420℃. Moreover, compared with Li2S, the main characteristic peak intensity of Li-argyrodite is higher, and it takes up the main position in phase composition. A same situation also appears in Li6PS5Cl0.9I0.1 (Figure S6a) and Li6PS5Cl0.8I0.2 (Figure S6b), Li-argyrodite phase also first appear at 100℃, and more obviously, with the increase of LiI doping amount, and the peak intensity of Li2S gradually decreases. The above results are similar to those obtained by predecessors[28, 37]. The above results indicate that doping LiI can help to form the phase at a lower temperature and reduce the raw material phase of Li2S in the argyrodite.

Figure 5. (a) The cycling performance, (b) charge-discharge curves, (c) rate performance of NCM622/ Li6PS5Cl0.95I0.05 /graphite ASSLBs.

In order to know the electrochemical properties of the I0.05-LPSC SSEs, the all-solid-state batteries by combining NCM622 cathode and graphite anode with Li6PS5Cl0.95I0.05 were assembled to assess the performance of the electrolytes. All of the batteries were tested by charging and discharging between 3 and 4.2 V at the loading of 18.7 mg cm-2. The cycling performance of the NCM622/ I0.05-LPSC /Gr battery at various C-rates are presented in Figure 5a. The reversible discharge capacities for NCM622/ I0.05-LPSC /Gr battery at 0.1, 0.3, 0.5 and 1 C are 151.1, 135.8, 124.9, 105.2 mAh·g-1, respectively, then a capacity of 134.8 mAh·g-1 can be obtained at 0.3C, demonstrating excellent rate performance. Figure 5b displays the charge-discharge curves of NCM622/ I0.05-LPSC /Gr ASSLB, the charge capacity of the first circle is 195.8 mAh·g-1 at 0.1 C, the specific discharge capacity is 150.8 mAh·g-1, and the Coulomb efficiency is 77%. Finally, figure 5c shows the long cycling stability of ASSLB, the charge and discharge test of the first three circles at 0.1 C (0.28 mA·cm-2), and the next charge and discharge test at 0.3 C, the battery exhibits a specific discharge capacity of 128.9 mAh·g-1 during a long cycle, and a capacity retention rate of 97.9% at 0.3C after 100 cycles.

- Conclusions

In summary, in the case of direct powder mixing without raw material treatment, LPSC synthesis will produce a large Li2S impurity peak, but the addition of LiI will effectively inhibit the production of impurity phases. Moreover, without I doping, LPSC needs to be heated to 550 ℃ to obtain high conductivity of 4.3 mS·cm-1, but after adding only 5% mol LiI, this temperature is reduced to 480 ℃, and the Li6PS5Cl0.09I0.05 electrolyte with a conductivity of 3.91 mS·cm-1 is obtained. In situ XRD test shows that the argyrodite LPSC phase of the LiI-doped precursor has already appeared at 100 ℃, while the original LPSC requires up to 450 ℃, indicating that LiI greatly reduces the phase forming temperature of LPSC synthesis. These results indicate that the doping of LiI can promote synthesis of the argyrodite LPSC. Furthermore, the obtained Li6PS5Cl0.95I0.05 electrolyte was employed in NCM622/ I0.05-LPSC /Gr batteries, delivering a 97.9% retention rate after 100 cycles. Therefore, these results prove that a small amount of LiI doping is a promising strategy in the preparation of large quantities to LPSC.

[1] C. Yu, F.P. Zhao, J. Luo, L. Zhang, X.L. Sun, Recent development of lithium argyrodite solid-state electrolytes for solid-state batteries: Synthesis, structure, stability and dynamics, Nano Energy 83 (2021).

[2] B.Z. Zheng, X.S. Liu, J.P. Zhu, J. Zhao, G.M. Zhong, Y.X. Xiang, H.C. Wang, W.M. Zhao, E. Umeshbabu, Q.H. Wu, J.Y. Huang, Y. Yang, Unraveling (electro)-chemical stability and interfacial reactions of Li10SnP2S12 in all-solid-state Li batteries, Nano Energy 67 (2020).

[3] Z.R. Zhang, J.X. Zhang, Y.L. Sun, H.H. Jia, L.F. Peng, Y.Y. Zhang, J. Xie, Li4-xSbxSn1-xS4 solid solutions for air-stable solid electrolytes, J. Energy Chem. 41 (2020) 171-176.

[4] N. Seitzman, H. Guthrey, D.B. Sulas, H.A.S. Platt, M. Al-Jassim, S. Pylypenko, Toward All-Solid-State Lithium Batteries: Three-Dimensional Visualization of Lithium Migration in beta-Li3PS4 Ceramic Electrolyte, J. Electrochem. Soc. 165(16) (2018) A3732-A3737.

[5] H. Liu, Q. Zhu, C. Wang, G. Wang, Y. Liang, D. Li, L. Gao, L.Z. Fan, High Air Stability and Excellent Li Metal Compatibility of Argyrodite‐Based Electrolyte Enabling Superior All‐Solid‐State Li Metal Batteries, Advanced Functional Materials 32(32) (2022).

[6] S.J. Liu, L. Zhou, J. Han, K.H. Wen, S.D. Guan, C.J. Xue, Z. Zhang, B. Xu, Y.H. Lin, Y. Shen, L.L. Li, C.W. Nan, Super Long-Cycling All-Solid-State Battery with Thin Li6PS5Cl-Based Electrolyte, Adv. Energy Mater. 12(25) (2022) 9.

[7] Y. Wang, J. Ju, S. Dong, Y. Yan, F. Jiang, L. Cui, Q. Wang, X. Han, G. Cui, Facile Design of Sulfide‐Based all Solid‐State Lithium Metal Battery: In Situ Polymerization within Self‐Supported Porous Argyrodite Skeleton, Advanced Functional Materials 31(28) (2021).

[8] C. Luo, X. Ji, J. Chen, K.J. Gaskell, X. He, Y. Liang, J. Jiang, C. Wang, Solid-State Electrolyte Anchored with a Carboxylated Azo Compound for All-Solid-State Lithium Batteries, Angew Chem Int Ed Engl 57(28) (2018) 8567-8571.

[9] R.P. Rao, S. Adams, Membranes for rechargeable lithium sulphur semi-flow batteries, J. Mater. Sci. 51(11) (2016) 5556-5564.

[10] H. Kitaura, A. Hayashi, K. Tadanaga, M. Tatsumisago, Electrochemical Analysis of Li4Ti5O12 Electrode in All-Solid-State Lithium Secondary Batteries, J. Electrochem. Soc. 156(2) (2009) A114-A119.

[11] X. Li, J. Liang, J. Luo, C. Wang, X. Li, Q. Sun, R. Li, L. Zhang, R. Yang, S. Lu, H. Huang, X. Sun, High-Performance Li-SeSx All-Solid-State Lithium Batteries, Adv Mater 31(17) (2019) e1808100.

[12] H. Lee, P. Oh, J. Kim, H. Cha, S. Chae, S. Lee, J. Cho, Advances and Prospects of Sulfide All-Solid-State Lithium Batteries via One-to-One Comparison with Conventional Liquid Lithium Ion Batteries, Adv Mater 31(29) (2019) e1900376.

[13] H. Takahara, T. Takeuchi, M. Tabuchi, H. Kageyama, Y. Kobayashi, Y. Kurisu, S. Kondo, R. Kanno, All-solid-state lithium secondary battery using oxysulfide glass - Addition and coating of carbon to positive electrode, J. Electrochem. Soc. 151(10) (2004) A1539-A1544.

[14] P. Oh, H. Lee, S. Park, H. Cha, J. Kim, J. Cho, Improvements to the Overpotential of All-Solid-State Lithium-Ion Batteries during the Past Ten Years, Adv. Energy Mater. 10(24) (2020) 8.

[15] K. Lee, J. Lee, S. Choi, K. Char, J.W. Choi, Thiol-Ene Click Reaction for Fine Polarity Tuning of Polymeric Binders in Solution-Processed All-Solid-State Batteries, ACS Energy Lett. 4(1) (2019) 94-101.

[16] Z.X. Zhang, L. Zhang, X.L. Yan, H.Q. Wang, Y.Y. Liu, C. Yu, X.T. Cao, L. van Eijck, B. Wen, All-in-one improvement toward Li6PS5Br-Based solid electrolytes triggered by compositional tune, J. Power Sources 410 (2019) 162-170.

[17] G.F. Dewald, S. Ohno, M.A. Kraft, R. Koerver, P. Till, N.M. Vargas-Barbosa, J. Janek, W.G. Zeier, Experimental Assessment of the Practical Oxidative Stability of Lithium Thiophosphate Solid Electrolytes, Chem. Mater. 31(20) (2019) 8328-8337.

[18] I. Hanghofer, B. Gadermaier, H.M.R. Wilkening, Fast Rotational Dynamics in Argyrodite-Type Li6PS5X (X: CI, Br, I) as Seen by P-31 Nuclear Magnetic Relaxation On Cation Anion Coupled Transport in Thiophosphates, Chem. Mater. 31(12) (2019) 4591-4597.

[19] I. Hanghofer, M. Brinek, S.L. Eisbacher, B. Bitschnau, M. Volck, V. Hennige, I. Hanzu, D. Rettenwander, H.M.R. Wilkening, Substitutional disorder: structure and ion dynamics of the argyrodites Li6PS5Cl, Li6PS5Br and Li6PS5I, Phys Chem Chem Phys 21(16) (2019) 8489-8507.

[20] A.R. Stamminger, B. Ziebarth, M. Mrovec, T. Hammerschmidt, R. Drautz, Ionic Conductivity and Its Dependence on Structural Disorder in Halogenated Argyrodites Li6PS5X (X = Br, Cl, I), Chemistry of Materials 31(21) (2019) 8673-8678.

[21] N. Minafra, S.P. Culver, T. Krauskopf, A. Senyshyn, W.G. Zeier, Effect of Si substitution on the structural and transport properties of superionic Li-argyrodites, J. Mater. Chem. A 6(2) (2018) 645-651.

[22] N.C. Rosero-Navarro, A. Miura, K. Tadanaga, Composite cathode prepared by argyrodite precursor solution assisted by dispersant agents for bulk-type all-solid-state batteries, J. Power Sources 396 (2018) 33-40.

[23] C. Yu, J. Hageman, S. Ganapathy, L. van Eijck, L. Zhang, K.R. Adair, X.L. Sun, M. Wagemaker, Tailoring Li6PS5Br ionic conductivity and understanding of its role in cathode mixtures for high performance all-solid-state Li-S batteries, J. Mater. Chem. A 7(17) (2019) 10412-10421.

[24] Y.X. Wang, D.P. Lu, J. Xiao, Y. He, G.J. Harvey, C.M. Wang, J.G. Zhang, J. Liu, Superionic conduction and interfacial properties of the low temperature phase Li7P2S8Br0.5I0.5, Energy Storage Mater. 19 (2019) 80-87.

[25] Y. Bai, Y.B. Zhao, W.D. Li, L.H. Meng, Y.P. Bai, G.R. Chen, New Insight for Solid Sulfide Electrolytes LSiPSI by Using Si/P/S as the Raw Materials and I Doping, ACS Sustainable Chem. Eng. 7(15) (2019) 12930-12937.

[26] H. Wang, C. Yu, S. Ganapathy, E.R.H. van Eck, L. van Eijck, M. Wagemaker, A lithium argyrodite Li6PS5Cl0.5Br0.5 electrolyte with improved bulk and interfacial conductivity, J. Power Sources 412 (2019) 29-36.

[27] H. Chen, Y. Lu, H. Zhang, Y. Zhou, J. Chen, X. Huang, B. Tian, 20 mS cm−1 Li-argyrodite solid electrolyte produced via facile high-speed-mixing, Chemical Communications 59(47) (2023) 7220-7223.

[28] S. Ujiie, A. Hayashi, M. Tatsumisago, Preparation and ionic conductivity of (100-x)(0.8Li(2)S center dot 0.2P(2)S(5))center dot xLiI glass-ceramic electrolytes, J. Solid State Electrochem. 17(3) (2013) 675-680.

[29] Z.X. Zhang, L. Zhang, Y.Y. Liu, C. Yu, X.L. Yan, B. Xu, L.M. Wang, Synthesis and characterization of argyrodite solid electrolytes for all-solid-state Li-ion batteries, J. Alloys Compd. 747 (2018) 227-235.

[30] S. Yubuchi, S. Teragawa, K. Aso, K. Tadanaga, A. Hayashi, M. Tatsumisago, Preparation of high lithium-ion conducting Li6PS5Cl solid electrolyte from ethanol solution for all-solid-state lithium batteries, J. Power Sources 293 (2015) 941-945.

[31] Z. Zhang, Y. Tian, G. Liu, M. Wu, H. He, X. Yao, Superionic Lithium Argyrodite Electrolytes by Bromine-Doping for All-Solid-State Lithium Batteries, Journal of The Electrochemical Society 169(4) (2022).

[32] S. Yubuchi, H. Tsukasaki, A. Sakuda, S. Mori, A. Hayashi, M. Tatsumisago, Quantitative analysis of crystallinity in an argyrodite sulfide-based solid electrolyte synthesized via solution processing, RSC Adv 9(25) (2019) 14465-14471.

[33] Y. Subramanian, R. Rajagopal, S. Kang, K.-S. Ryu, Enhancement of lithium argyrodite interface stability through MoO2 substitution and its application in lithium solid state batteries, Journal of Alloys and Compounds 925 (2022).

[34] R.C. Xu, F.D. Han, X. Ji, X.L. Fan, J.P. Tu, C.S. Wang, Interface engineering of sulfide electrolytes for all-solid-state lithium batteries, Nano Energy 53 (2018) 958-966.

[35] S. Wenzel, S.J. Sedlmaier, C. Dietrich, W.G. Zeier, J. Janek, Interfacial reactivity and interphase growth of argyrodite solid electrolytes at lithium metal electrodes, Solid State Ionics 318 (2018) 102-112.

[36] R.P. Rao, S. Adams, Studies of lithium argyrodite solid electrolytes for all-solid-state batteries, Physica Status Solidi a-Applications and Materials Science 208(8) (2011) 1804-1807.

[37] T. Ohtomo, A. Hayashi, M. Tatsumisago, K. Kawamoto, Glass Electrolytes with High Ion Conductivity and High Chemical Stability in the System LiI-Li2O-Li2S-P2S5, Electrochemistry 81(6) (2013) 428-431.